## Slide 1
Materials Data in Action

## Slide 2: Predicting the formation of binary compounds using machine learning
Chris Borg, Research Scientist
5 September 2019

## Slide 3: Agenda
0. Is this a good problem for ML?
Data preparation
Modeling
  Classification with random forest
  Model quality metrics
Compare to DFT
  Model performance vs. “ground-truth”
Further considerations
Notes: https://citrination.com/datasets/181017/show_search?searchMatchOption=fuzzyMatch

## Slide 4: Task: Predict the stability of binary compounds
Task: build a machine learning model in Python to predict the full stability vector
stabilityVec: [1, 0, 0, 0, 0, 1, 1, 0, 0, 0, 1]
Na, NaCl, Na2Cl3, Cl
http://oqmd.org/materials/composition/NaCl
1 = stable
0 = unstable
Typically, chemists use thermodynamics to determine the relative stability of a binary (AB) compound.
Notes: https://citrination.com/datasets/181017/show_search?searchMatchOption=fuzzyMatch
delH = enthalpy of formation.

## Slide 5: Is this a reasonable problem for ML to solve?
Machine learning (ML): A set of data-driven algorithms that discern patterns from high-dimensional spaces.
High-dimensional input space: chemical composition (can be mapped to 100s of physically meaningful features)
Binary output: stable/unstable labels for 68k compositions (82 elements, 2572 AB combinations)
Validation / ”ground-truth”: DFT calculated enthalpies of formation
Notes: (i.e. do we believe our output of interest in controlled by more than 3 variables?)

## Slide 6: Preparing dataset
…
2572 rows, 99 columns: element A, element B, stability vector, 48 features per element (A, B)
Each row is now a single composition (input) and stability classification (output)
Inputs:
Output:
Input:
Output:
Notes: https://citrination.com/datasets/181017/show_search?searchMatchOption=fuzzyMatch

## Slide 7: Deriving physically-informed features
Notes: https://citrination.com/datasets/181017/show_search?searchMatchOption=fuzzyMatch

## Slide 8: Choosing an estimator
Random forest
Interpretable (ranked feature importance)
Can capture non-linear correlations
5144 stable monatomic
2493 stable binaries
20655 unstable binaries
random guess = 0.5
”intuition” = 0.82
Establishing a baseline:
Notes: https://citrination.com/data_views/11942/predict

## Slide 9: Evaluating predictions
 | N (predicted) | P (predicted)
N (actual) | TN = 6665 | FP = 173
P (actual) | FN = 583 | TP = 1916
Accuracy
3-fold CV avg. accuracy = 0.963
10-fold CV avg. accuracy = 0.967
F1 score = 0.84
Notes: # precision: What proportion of positive identifications was actually correct?
precision = tp/(tp+fp)
# recall: What proportion of actual positives was identified correctly?
recall = tp/(tp+fn)
2 * (precision * recall) / (precision + recall)

## Slide 10: Graphical model accuracy metrics
Typically, an ROC curve is a good measure of the ability of a binary classifier.
However this is an overly optimistic view due to the large class imbalance between stable and unstable compounds. PR curve better captures the classification ability of the model.
AUROC = 0.96
AP = 0.78
Notes: https://citrination.com/data_views/11942/predict

## Slide 11: Comparing against DFT
Added DFT calculated stability to test data.
While accuracy is high, FP is more than 2x TP.
If a researcher were to attempt synthesis of predicted compounds, they may likely succeed 50% of the time.
 | N (predicted) | P (predicted)
N (actual) | TN = 6230 | FP = 218
P (actual) | FN = 196 | TP = 97
Accuracy = 0.94
F1 score = 0.32
Notes: https://citrination.com/data_views/11942/predict
GS = dft volume per atom

## Slide 12: Important features
“The Mendeleev number (MN) (ordering number listing the chemical elements column by column through the periodic system) was successfully used to classify the chemical systems”
Notes: https://citrination.com/data_views/11942/predict
GS = dft volume per atom

## Slide 13: Conclusions
The random forest model trained on the given data is able to discern, above a baseline, between stable and unstable compounds.
However, the class imbalance (low number of stable compounds) skews our perspective on the model’s classification ability (as shown in the comparison to DFT)
This imbalance causes an equivalent number of false positives and false negatives and could be address through re-samples (super- or sub- sampling)
Notes: https://citrination.com/data_views/11942/predict
GS = dft volume per atom

## Slide 14: Logistic regression results
AP = 0.65
AUROC = 0.913
 | N (predicted) | P (predicted)
N (actual) | TN = 6395 | FP = 443
P (actual) | FN = 681 | TP = 1818
Accuracy = 0.88
F1_score = 0.76
 | N (predicted) | P (predicted)
N (actual) | TN = 6046 | FP = 402
P (actual) | FN = 199 | TP = 94
Held out test set
DFT-labeled test_data.csv
Accuracy = 0.911
F1_score = 0.24
Notes: https://citrination.com/data_views/11942/predict
GS = dft volume per atom

## Slide 15: rf supersampled
 | N (predicted) | P (predicted)
N (actual) | TN = 6483 | FP = 412
P (actual) | FN = 29 | TP = 4881
Accuracy = 0.96
F1_score = 0.96
 | N (predicted) | P (predicted)
N (actual) | TN = 5897 | FP = 551
P (actual) | FN = 126 | TP = 167
Held out test set
DFT-labeled test_data.csv
Accuracy = 0.9
F1_score = 0.33
AUROC = 0.996
AP = 0.92
Notes: https://citrination.com/data_views/11942/predict
GS = dft volume per atom

## Slide 16: Further considerations
Investigate design space, low F1 score could be due to inability to extrapolate
Feature engineering
More data
Notes: https://citrination.com/data_views/11942/predict
GS = dft volume per atom

## Slide 17
THANK YOU!

## Slide 18: Tuning rf hyperparameters
n_estimators = 10 | N (predicted) | P (predicted)
N (actual) | TN = 6665 | FP = 173
P (actual) | FN = 583 | TP = 1916
n_estimators = 20 | N (predicted) | P (predicted)
N (actual) | TN = 6697 | FP = 141
P (actual) | FN = 578 | TP = 1921
n_estimators = 3 | N (predicted) | P (predicted)
N (actual) | TN = 6500 | FP = 338
P (actual) | FN = 539 | TP = 1960
test_size = 0.1 | N (predicted) | P (predicted)
N (actual) | TN = 2002 | FP = 50
P (actual) | FN = 160 | TP = 618
test_size = 0.25 | N (predicted) | P (predicted)
N (actual) | TN = 5126 | FP = 102
P (actual) | FN = 405 | TP = 1440
test_size = 0.33 | N (predicted) | P (predicted)
N (actual) | TN = 6665 | FP = 173
P (actual) | FN = 583 | TP = 1916
Notes: https://citrination.com/data_views/11942/predict

## Slide 19: Binary classification on Citrination
Random subset of data (Citrination limit = 4k rows)
AUROC = 0.948
Notes: https://citrination.com/datasets/181017/show_search?searchMatchOption=fuzzyMatch

## Slide 20: Test case: Na, Cl
Actual: [1, 0, 0, 0, 0, 1, 1, 0, 0, 0, 1]
http://oqmd.org/materials/composition/NaCl
compound | stable | unstable
Na | 1 | 0
Na0.9 | 0.14 | 0.86
Na0.8 | 0.22 | 0.78
Na0.7 | 0.25 | 0.75
Na0.6 | 0.31 | 0.69
Na0.5 | 0.35 | 0.65
Na0.4 | 0.21 | 0.79
Na0.3 | 0.13 | 0.87
Na0.2 | 0.07 | 0.93
Na0.1 | 0.05 | 0.95
Cl | 1 | 0
Predicted: [1, 0, 0, 0, 0, 0, 0, 0, 0, 0, 1]
Conclusion: No better than random, worse than intuition
Notes: https://citrination.com/data_views/11942/predict